## Slide 1: Templating Ion-Conducting Membranes Using Block Copolymers
TEM
SEO:LiClO4 3:1
SEO neat
Scale bar : 20 nm
RuO4 staining
SAXS
q (Å-1)
Log Intensity (a.u.)
√3
√3
√7
√7
√7
2
3
4
1
1
1
1
1
√4
√4
√9
√9
1
[EO]:[Li]
q/q* =
We have investigated the self-assembly of cylinder-forming PS-b-PEO (SEO) block copolymers doped with various lithium salts. SAXS and TEM confirm that salt doping increases the domain spacing and segregation strength. Additionally, the lithium counterion is shown to affect the morphologies and induces unique thermal phase transitions.