## Slide 1
Hybrid NP/POM films prepared using LbL assembly are ‘modular’, offering the possibility to study a wide variety of POMs and nanoparticles using the same thin film architecture.
Improved Oxygen Reduction Cathodes Using Polyoxometalate Cocatalysts
YES! POMs with weaker M-O bonds (Co) exhibit a greater influence on oxygen reduction at Au surfaces (i.e., a more positive shift of the potential) than POMs with stronger M-O bonds.
O2 + 4e– + 4H+ === 2H2O (1)
2M + O2 === 2MO (2)
2MO +4e– + 4H+ === 2H2O (3)
Taking oxygen reduction as our paradigm case, can polyoxometalate (POM) nanoparticle hybrid thin films provide insight into the behavior of multimetallic electrocatalysts?
Sankarraj, Ramakrishnan, Shannon, Langmuir, 2008, 24, 632; Xin, Shannon, Langmuir, submitted.
PI: C. Shannon, Auburn University
ORR specific activities of about 7 mA/cm2 have been observed, exceeding the activity of commercial Pt/C catalysts by an order of magnitude