## Slide 1
Adsorption-Induced Changes in Zeolite Membrane Structures
John L. Falconer, Department of Chemical and Biological Engineering, University of Colorado, Boulder, CO
Zeolite A membranes are selective for water/alcohol liquid separations, but they have poor gas selectivities due to the presence of intercrystalline regions (defects) in the polycrystalline membranes. Permporosimetry measurements shown on the right and depicted schematically below, indicate that water and methanol swell the zeolite A crystals and thus reduce flow through defects, but isopropanol and ethanol do not, and this swelling may be partly responsible for the high selectivities observed in pervaporation.
Zeolite Crystals
Porous Support
He flow through crystals
He flow through defects
He flow through crystals
He defect flow reduced
+ H2O or MeOH

## Slide 4
The reduction in flow is thought to be a result of expansion of the zeolite crystals which causes the defects to shrink, thereby reducing defect transport.