## Slide 1
Synthesis and Characterization of Novel Donor/Acceptor Molecules
Based on Propellanes: A Probe of Nonclassical Conjugation
Frankie Ann McCormick
Department of Chemistry, Northern Michigan University
Unique donor/acceptor molecules (I) based on the 1,3-di-ethynylbicyclo[1.1.1]pentane (diethynylpropellane) spacer are being investigated to probe nonclassical conjugation through the propellane unit. The work represents the first experimental study of charge transfer from donor (D) to acceptor (A) through chromophores linked by diethynyl-propellane. We plan to synthesize and study the spectro-scopic behavior of a series of targets with different combinations of D/A groups. The extent of interaction will be characterized by UV-vis and fluorescence spec-troscopy. These molecules may find potential applications in molecular electronics, optics, and photovoltaic devices.
We have prepared four of the targets using sequential palladium coupling to the parent 1,3-diethynyl-propellane: charge transfer is evident in the three systems characterized by UV-vis spectroscopy and preliminary fluorescence data suggest an intense, broad, red-shifted CT emission for Ia at 618 nm upon excitation at 285 nm.
UV-vis spectra in Dioxane:
D A l max (nm)
__________________________________________________________________________________________________________________________
Ia OMe CN 284
Ib NMe2 CN 288
Ic NMe2 NO2 296
diethynylpropellane -