## Slide 1: On the activation mechanism of Sn to the EER of ethanol: decomposition of H2O and ethanol over PtnM clusters Yixuan Wang, Albany State University, Albany, GA 31705
A two layer cluster with 7 atoms on the surface and 3 atoms on the second layer, has been used to model Pt-M alloy surface. Relative to the adsorbed water, it is interesting to find that thermodynamically and kinetically the decomposition of the adsorbed water on Sn site is more favorable than the decomposition on Pt and Ru sites. Taking Pt as a reference, the plot of relative Ea against relative Ediss for water dissociation over the investigated transition metals M (Pd, Ru, Rh, Cu, Sn, and Re) is illustrated. According to the plot, the bimetallic alloys PtM (M=Re, Sn and Ru) are more active to water dissociation both kinetically and thermodynamically, while the bimetals alloying with Cu, Pd and Rh are less active than Pt from both aspects. This result supports the assumption of the bi-functional mechanism, where Sn site facilitates the dissociation of H2O.
The fundamental assumption of the bi-functional mechanism for PtSn alloy to catalyze ethanol electro-oxidation reaction is that Sn facilitates the dissociation of H2O and Pt site catalyzes ethanol decomposition. Our investigation is to clarify this assumption and get detailed information about decomposition mechanism of H2O and CH3CH2OH.
The relative dissociation energy against the relative energy barrier for water dissociation over the M site of Pt9M.
External electric fields were added into DFT calculations of H2O-PtnM (n=6 and 9; M=Pt, Sn and Ru). Although activation energies over Pt6M have the opposite change to those over Pt9M, PtSn still exhibits the most active kinetically to water decomposition among the three clusters.