## Slide 1: Simultaneous Increase in Seebeck Coefficient and Conductivity in a Doped Poly(alkylthiophene) Blend with Defined Density of States H.E. Katz, Johns Hopkins University, and A. Majumdar, University of California, Berkeley
Seebeck coefficient, a defining parameter for thermoelectric materials, depends on the contributions to conductivity of charge carriers at energies away from the Fermi level. Highly conductive materials tend to exhibit conductivity from carriers close to the Fermi level. Here, we report polymer blends in which ground state hole carriers, created by doping a minor additive component, are mainly at an orbital energy set below the hole energy of the major component of the blend. Transport, however, is expected to occur through the major component. This leads to a regime in which hole conductivity and Seebeck coefficient may be increased in parallel. While the absolute conductivity of the composite, and thus ZT, are not particularly high, this work demonstrates a route for designing thermoelectric materials in which increases in Seebeck coefficient and conductivity do not cancel each other. The plots of Seebeck coefficient and conductivity in the graphic feature a regime on the left in which both parameters increase simultaneously, as the theory predicts.