## Slide 1
Catalyst Engineering Using Support-Dopant Modification: Towards Intelligent Design of Catalyst Systems
Ryan O’Hayre, Department of Metallurgical and Materials Engineering, Colorado School of Mines
Motivation: Exploit a novel surface-modification technique to enhance the catalytic activity and durability of Pt/C systems relevant to fuel cell applications. Determine the fundamental mechanisms that underpin this effect.
Approach: Our experimental approach uses highly controlled, geometrically simple Pt/graphite test-systems. The fundamental mechanisms and effects of surface dopant modification are explored by comparing the structure, chemistry, and activity of doped versus undoped (control) catalyst systems (fig 1).
Figure 1. Our experimental approach
Results: Using SEM imaging combined with statistical image analysis methods, we have shown that N-modified graphite surfaces lead to significantly smaller average catalyst particle size and a narrower catalyst size distribution compared to alternative dopants (fig 2). Using electrochemical techniques (IV, CV, EIS), we have shown that 10% surface N-modification appears to lead to optimal catalytic activity (fig 3).
Figure 3. N-doping provides the best results (small, homogenous catalyst particles)
Figure 2. 45 sec nitrogen-doping (10% N loading) leads to best catalytic performance.