## Slide 1
A New Type of Discotic Liquid Crystals for Organic Solar Cells
Liang-shi Li, Department of Chemistry, Indiana University, Bloomington IN 47405
Colloidal Graphene Quantum Dots: Solution-processable organic semiconductors are important components in low-cost electronics including photovoltaics, light emitting diodes, and field effect transistors. However, the low electrical conductivity of the common solution-processable organic semiconductors has been a factor limiting the device performance.
Our goal is to develop a new type of discotic semiconductors for organic solar cells. Processed with solution-based methods, the liquid crystals can have long-range supramolecular order and thus can transport charges with large speed. In addition, the compounds we target will have the ability to simultaneously optimize photoinduced charge separation and the subsequent charge transport to electrodes, and therefore are ideal for fabricating organic solar cells.
We have developed a new class of discotic semiconductors - colloidal graphene quantum dots (e.g., 1), which are primarily made of carbon, an abundant element on earth, and have superior electro-optical properties for solar energy conversion. For example, Due to its large size, 1 absorbs sunlight with wavelength shorter than 900 nm (absorption spectrum shown below), the optimum value for single-junction solar cells under non-concentrated light.
Their large solubility in common solvents allows us to process the graphene quantum dots from solution. We have demonstrated that 1 can be used as an effective light absorber in dye-sensitized solar cells.