## Slide 1: Hybrid Structures of Photonic Crystals & Mesoporous Films
As a chemical (TMOS) is infiltrated into the pores of the mesoporous layer, sandwiched between two photonic crystals, the defect peak red-shifts.
substrate
Photonic
Crystal
Mesoporous Film
Photonic
Crystal
The hybrid structure is fabricated by embedding a mesoporous layer in between two photonic crystals made up of silica spheres. The mesoporous layer acts as a defect layer, transmitting light at a specific wavelength that was previously forbidden. This is exhibited as a dip in the reflectivity spectrum.