## Slide 1
Understanding the Diffusion of Polymers Confined Between Interfaces
Christopher J. Ellison, Department of Chemical Engineering, University of Texas at Austin
Whole chain polymer mobility at and near interfaces has significant implications in the fabrication of microelectronics using polymeric photoresists and in polymeric surfactants used in flooding for tertiary oil-recovery. While many studies focus on diffusion perpendicular to a substrate, little is known about in-plane diffusion which we aim to study here. Using covalently labeled fluorescent polymers and fluorescence recovery after photobleaching (FRAP) we are able to directly measure the diffusion of polymers parallel to the substrate in thin films. This technique allows us to control the film thickness, temperature, molecular weight, surface energy and substrate interactions independently.
Before
After
Chart: Time (seconds)
| 0 | 780.32799999999975 | 1024.422 | 1268.8119999999999 | 1513.25 | 1757.6869999999999 | 2002.1869999999999 | 2246.578 | 2491.0149999999999 | 2735.4679999999998 | 2979.9059999999999 | 3224.3589999999999 | 3468.797 | 3713.2339999999999 | 3957.686999999999 | 4202.1250000000018 | 4446.5620000000017 | 4691.0150000000003 | 4935.4530000000004 | 5179.9059999999999 | 5424.3430000000008 | 5668.7809999999999 | 5913.2339999999995 | 6157.6720000000014 | 6402.1090000000004 | 6646.5620000000017 | 6891 | 7135.4370000000008 | 7379.89 | 7624.3280000000004 | 7868.7809999999999 | 8113.2179999999998 | 8357.6720000000005 | 8602.1090000000004
Data | 0 | 0.18011 | 0.25359 | 0.30665 | 0.33813 | 0.38842 | 0.39357 | 0.43264 | 0.44881 | 0.49861 | 0.48348 | 0.49976 | 0.54601 | 0.54198 | 0.57695 | 0.61283 | 0.63206 | 0.628 | 0.62866 | 0.67878 | 0.65247 | 0.68811 | 0.65198 | 0.67342 | 0.69407 | 0.71727 | 0.73659 | 0.74097 | 0.79 | 0.72644 | 0.78707 | 0.75264 | 0.78256 | 0.79158
PiBMA-NBD