## Slide 1
Characterizing and Directing the Initial Dynamics in Multi-Component Solar Powered Water-Splitting Inorganic Photocatalysts
Delmar s Larsen, Department of Chemistry, University of California, Davis
Hydrogen is an environmentally benign fuel for the generation of power, heat, and electricity. Photocatalytic H2O splitting has received considerable attention as a solar energy driven pathway to hydrogen generation. Thermodynamically visible light is sufficiently energetic to lead to direct H2O splitting, which exhibits a 1.23 eV difference of its coupled half-reactions. Yet this is not observed in any great yield, in part due to the rapid recombination of photogenerated charge carriers leading to low quantum yields associated with the visible spectrum. Thus, materials must be engineered to enhance charge separated lifetimes of electron-hole pairs allowing solar energy to be stored in the form of H2 through the decomposition of H2O.
Hydrogen evolution with 10 mg of CdSe nanocatalysts in H2O and 0.1M Na2S:Na2SO3 under visible irradiation (λ > 400nm) from a 300W Xe lamp. Linear fits are shown with data. QD=Quantum Dots and NR- NanoRibbons
Wavelength (nm)
Time (ps)
450
500
550
600
650
700
0
2.5
5
50
500
5000
-6
-5
-4
-3
-2
-1
0
1
2
Wavelength (nm)
Time (ps)
450
500
550
600
650
700
0
2.5
5
50
500
5000
-2
-1
0
1
2
3
CdSe QD/Water (post-dialysis) Photodynamics
CdSe QD/Water (pre-dialysis) Photodynamics